|  | COUNTY OF DANE DEPARTMENT OF ADMINISTRATION PURCHASING DIVISION Room 425 City-County Building 210 Martin Luther King Jr. Blvd. Madison, WI 53703-3345 608-266-4131 FAX 608-266-4425 TDD 608-266-4941 |  |
| --- | --- | --- |
| CARLOS PABELLON Director of Administration |  | CHARLES HICKLIN Controller |

DATE:		March 28, 2017

TO:	All Proposers BID #117034 – HMA & Cold Mix Pavement Projects

# FROM:		Pete Patten, Purchasing Agent

SUBJECT:		ADDENDUM #1

After the pre-bid meeting, the specifications listed below have been revised. Please use the revised bid specifications and price proposal from this addendum when submitting your proposal.

Additions/revisions are shown in red in the document.

Please acknowledge receipt of this addendum by noting “Addendum #1 Received” on the bottom of the Signature Affidavit when you submit your bid. If you have any questions regarding this addendum, please contact me at 608-267-3523.

Sincerely,

Pete Patten

Purchasing Agent

###### Part 3 – Detailed Specifications

###### Submit with Bid

HMA & COLD MIX PAVEMENT SPECIFICATIONS

Bids must be submitted on the attached RFB forms. Dane County reserves the right to accept or reject any and all bids submitted; and to accept such bids deemed to be in the best interest of the County. The bids will be reviewed initially to determine if technical requirements are met.

GENERAL

All work and materials supplied under this proposal shall conform to the Standard Specifications for Road and Bridge Construction, 2017 edition (hereinafter referred to as the "Standard Specifications"), and all subsequent revisions and supplementary specifications, of the Wisconsin Division of Highways, Department of Transportation.

The special provisions in this proposal shall supplement and take precedence over the Standard Specifications.

The Dane County Highway and Transportation Department, the issuer of this bid proposal, shall hereinafter be referred to as "the County".  On certain projects, when specified on the schedule of prices, other municipalities or County agencies will be awarding and administering their own contract.

All projects included in this proposal are subject to available funds and budget restraints.

Bid Deposit/Performance Bond

Each proposal must be accompanied by a certified or cashier’s check payable to the Dane County Highway and Transportation Department, or by a bid bond, in the amount of 5% of the total amount bid.

# Successful bidders shall also furnish Dane County with a performance bond equal to 100% of the contracted amount (Wis. Statute 779.14)

# INSURANCE

Bidders shall carry insurance as required in the Standard Terms and Conditions, Section 20.  The bidder shall furnish Dane County Highway and Transportation Department along with the bid a certificate of insurance showing the type, amount, class of operations covered, effective dates, and expiration dates of policies.

CONTRACTOR QUALIFICATIONS

All contractors must meet the following requirements in order to bid:

- Have proven experience in highway paving and be included on the Wisconsin Department of Transportation list of prequalified contractors.

- Have equipment sufficient to produce, deliver, and pave 200 tons of asphaltic material per hour.

- Paving machines shall conform to the requirements of Section 450 of the Standard Specifications and be equipped with automatic leveling devices in working order.

- Paving machines shall have sufficient power, when paving widths of up to 16 feet, to maintain paving speed, alignment and grade.

- Experienced operators are required on all equipment used in the production and laying of the asphaltic material.

- The contractor shall provide to the County, upon request, a list of equipment to be used on these projects, along with certification as to capacities, etc.

- The following Emerging Small Business (ESB) requirements apply for all individual projects totaling $100,000 or more.  The contractor(s) submitting the responsible low bid shall provide required Emerging Small Business (ESB) reports to the Dane County Contract Compliance Officer within 24 hours after bid opening.  The Contract Compliance Officer can be contacted at (608) 266-5623 to obtain the required forms or if there are any questions regarding the ESB requirements.  If, upon evaluation of any of the bids submitted for any project over $100,000 the low bids bidder(s) are not awarded a contract, the next lowest responsible bidder(s) shall submit the required ESB reports within 24 hours of notification by the Contract Compliance Officer.

NOTICE TO BEGIN WORK

The contractor is required to begin work within ten calendar days after official notice from the County.  Liquidated damages of $200 per weekday will be assessed for any delay after this notification to begin.

The contractor will notify the County 48 hours in advance of beginning the project in order for the County to provide an inspector.  An inspector may not be furnished if notice of starting work by the contractor is not given to the County prior to 3:00 p.m. of the preceding day for projects starting on Tuesday thru Friday, or prior to 3:00 p.m. on Friday for projects starting on Saturday thru Monday.  Failure to notify the County could result in non-payment for that part of the work that is completed when an inspector is absent.

TERMINATION DATE

Asphaltic paving on these projects shall be terminated before November 15, 2017.  Any work performed beyond that date will be only by permission of the County.

PRODUCTION

On certain projects, when specified on the schedule of prices, the contractor shall supply a minimum of 200 ton per hour of asphaltic material on a continuous basis to provide a reasonable rate of production.  If the contractor falls below this rate, the County shall have the option of suspending work and liquidated damages of $300 per day will be assessed until full production is resumed.

After the asphaltic paving has started, the contractor shall proceed to complete the project at the earliest possible date.  If the contractor should determine it necessary to stop the paving operation, the contractor shall make a request to the County for permission to stop work.  The request shall be received by the County at least 24 hours before the proposed time of work stoppage.  The request shall specify the proposed date and time of work stoppage, the reason for stopping work, and the period of time before paving is to resume.  If permission is granted to discontinue work, the same liquidated damages as noted above will apply to further delays beyond the agreed resumption date.

The above conditions apply to all work on projects covered under this proposal.  Contractors or sub-contractors, whether performing paving, grinding, milling and shaping, or pulverizing, are expected to maintain normal progress.  Normal progress is defined as that which is reasonable for the scope of work involved.

TRUCK ROUTES

Hauling of asphalt paving material shall be done using County Class "A" highways and State highways, where possible.

TRAFFIC CONTROL

The contractor will be responsible for all traffic control, including furnishing and maintaining all signs, flags, flag-persons, barricades and lights where required, to protect the safety of the traveling public, all in accordance with Section 643 of the Standard Specifications, and the Federal Highway Administration, Manual on Uniform Traffic Control Devices and its supplements.  All work is to be done under traffic unless otherwise specified or allowed by the County.

REMOVING ASPHALT SURFACE MILLING, Item 204.0120

This work shall be in accordance with the requirements of Section 204 of the Standard Specifications, except as hereinafter amended.

- Description.  In most cases, milling will involve at least one vertical "butt" joint in order to match existing pavement.  Should topographic or other physical constraints prevent a milling machine from making a satisfactory straight line, vertical "butt" joint, the contractor shall provide all labor and equipment necessary to complete the joint by other means.

- Construction Methods.  When adjacent to an existing concrete gutter, the contractor shall "wedge" cut the existing pavement surface to a width as specified by the County.

The depth of the "wedge" cut shall be a minimum of 1 1/2 inches adjacent to the gutter and 1/8 inch on the outside edge towards the street centerline.  The depth of cut shall be measured to the top of the ridges.

- Method of Measurement.  Milling shall be measured by the square yard of pavement surface ground.  Widths of grinding greater than designated by the County shall be at the contractor's expense.

- Basis of Payment.  Milling will be paid for at the contract unit price bid for grinding, and shall be full compensation for grinding the existing pavement surface, constructing vertical butt joints, for wedging utility castings after grinding, for street cleaning, and for all equipment, tools, labor, and incidentals necessary to complete the work in accordance with this contract.

HMA PAVEMENT – ITEMS 460.5000 THRU 460.8999

A.	Description.  Materials covered under this provision shall conform to the State of Wisconsin, Department of Transportation's specifications for each “Type” mix.

The contractor will be responsible for providing mix design(s) and for testing required to insure uniformity of mix and adequacy of compaction.  A mix design must be submitted to the County for approval a minimum of 2 weeks prior to the start of paving.  In no case will paving be allowed to begin until the County is in receipt of said mix design(s).

## Section 460.2.1  Replace the entire text with the following:

      - Furnish a homogeneous mixture of coarse aggregate, fine aggregate, mineral filler if required, SMA stabilizer if required, recycled material if used, warm mix asphalt additive or process if used, and asphaltic material. Design mixtures conforming to table 460-1 and table 460-2 to 4.0% air voids to establish the aggregate structure.

      - Determine the target JMF asphalt binder content for production from the mix design data corresponding to 3.0% air voids (97% Gmm) target at the design the number of gyrations (Ndes). Add liquid asphalt to achieve the required air voids at Ndes.

      - For SMA, determine the target JMF asphalt binder content for production from the mix design data corresponding to 4.0% air voids (96% Gmm) target at Ndes.

B.	Method of Measurement.  Payment will be made only for supplied material accompanied by a ticket containing the following information:

1.  Ticket number, date, and time

2.  Type of material

3.  Gross and net weights

A copy of the tickets will be given to the County inspector on the job site.

C.	Basis of Payment.  HMA Pavement bid items is full compensation for providing HMA pavement including binder, accepted as stated above, compacted in place and shall include all work necessary to provide quality management programs in accordance with QMP Management Program (QMP) listed below.

Partial payments will be made no sooner than monthly by the County as the work proceeds.  Final payment will be withheld until final acceptance is made by the County.

D.	Acceptance.  Final acceptance of all asphaltic mixes shall be based primarily on the overall quality of finished pavement, compacted densities, the quality of workmanship and QMP documentation.  QMP Documentation must be turned into the County before final acceptance.  Documentation of the contractor's quality management program are definite factors in determining final acceptance, however the County reserves the right to reject any pavement on the basis of an obvious inconsistency, poor appearance, or poor ride.

Quality Management PROGRAM (QMP)

- Description.  The provisions of WisDOT Specification 460.2.8 (QMP) are removed from these specifications and replaced with the Specifications listed under field quality control.

- Field Quality Control:

- The Contractor is required to maintain an in-house Quality Control Program.  Contractor personnel must be qualified per section 8-36 of the WisDOT Construction and Materials Manual to run this program.  The engineer shall implement a Quality Assurance Program to reasonably assure that the specification are adhered to.  The Contractor shall notify the Engineer of Work stages as they progress.  The presence or absence of inspection or field observations shall not relieve the Contractor from inherent responsibility to conform to the specifications.

    - The contractor shall submit a proposed Job Mix Formula (JMF) for the Engineer’s review at a minimum of 2 weeks prior to paving.  The JMF shall be based on properties as specified by the Project’s Detailed Specifications.

    - A WisDOT HTCP Certified Mix Design Technician shall sign the JMF.  If certified personnel are not available, a Professional Engineer shall sign the above statement.

    - Mix designs must be preapproved by the Wisconsin Department of Transportation.

    - The Contractor shall take samples under their Quality Control Program.  For each mix produced, the contractor will sample and test as per the frequency requirements listed in the materials section of the QMP specifications.  Each sample shall be tested for gradation and air voids.  The average of all tests shall comply with the following specifications when compared to the JMF:

25.0 mm	+/- 6.0%

19.0 mm	+/- 5.0%

12.5 mm	+/- 5.0%

9.5 mm	+/- 5.0%

2.36 mm	+/- 5.0%

75-µm	+/- 2.0%

Asphaltic Content	+/- 0.3%

Air Voids	+/- 1.3%

VMA2	+/- 0.5%

2 VMA limits based on minimum requirement for mix design nominal maximum aggregate size in table 460-1.

- For each mix produced, the contractor shall submit one Asphalt Binder sample to be tested for compliance.  This sample shall be in a one quart can and clearly labeled.

- Testing Agency:  Contractor shall engage qualified testing agency to perform density tests.

- Thickness:  In place compacted thickness of hot-mix asphalt courses will be checked by Engineer.

- Surface Smoothness:  Finished surface of each hot-mix asphalt course will be observed by Engineer for compliance with smoothness tolerances.

- In-Place Density:  Testing agency will determine density using nuclear density methods.

  - Testing shall be performed the day of placement.

  - There shall be a minimum of five density tests for every 500 tons placed.  The five tests should be taken across the mat at  given location as may be designated by the Engineer.  The average of these five tests shall meet the minimum required density conforming to Table 460-3 of the WisDOT Specifications ASP-6.

TABLE 460-3  MINIMUM REQUIRED DENSITY[1]

| LOCATION | LAYER | PERCENT OF TARGET MAXIMUM DENSITY |
| --- | --- | --- |
|  |  | MIXTURE TYPE |
|  |  | LT and MT | HT | SMA[5] |
| TRAFFIC LANES[2] | LOWER UPPER | 93.0[3] 93.0 | 93.0[4] 93.0 93.0 |  |
| SIDE ROADS, | LOWER | 93.0[3] | 93.0[4] |  |
| CROSSOVERS, |  |  |  |  |
| TURN LANES & RAMPS | UPPER | 93.0 | 93.0 |  |
| SHOULDERS & | LOWER | 91.0 .0 | 91.0 .0 |  |
| APPURTENANCES | UPPER | 93.0 .0 | 92.0 .0 |  |

[1]  The table values are for average lot density. If any individual density test result falls more than 3.0 percent below the minimum required target maximum density, the engineer may investigate the acceptability of that material.

[2]  Includes parking lanes as determined by the engineer.

[3]  Minimum reduced by 2.0 percent for a lower layer constructed directly on crushed aggregate or recycled base courses.

[4] Minimum reduced by 1.0 percent for a lower layer constructed directly on crushed aggregate or recycled base courses.

[5] The minimum required densities for SMA mixtures are determined according to CMM-8-15.

  - Density tests will not be performed on leveling (scratch) courses.

- Mixtures with failing densities will be accepted and paid for as provided in WisDOT Section 460.5.2.2.

- Materials:  The Contractor will randomly take samples of the delivered asphalt mix to be tested for compliance with the mix design.

  - Frequency of Testing.  Daily sampling is required per each range of tonnage placed:  50-600 TN; 601-1,500 TN; 1,501-2,700 TN; 2,701-4200 TN.

  - Asphalt sample(s) to be tested for asphalt content, gradation, Bulk Specific Gravity (Gmb), Maximum Specific Gravity (Gmm), Air Voids (VA), Voids in Mineral Aggregates (VMA), and Percent Binder (Pb%).

- Materials:  The Contractor will randomly take samples of the delivered asphalt binder to be tested for compliance with the mix design.  The Contractor will take one test at a minimum one test per mix; testing for penetration and viscosity.

- Basis of Payment:  The contractor (bidder) shall include the Quality Management Program in the unit bid price for the asphaltic mixture.  Said bid price shall be full compensation for all work herein specified and for all labor, tools, equipment, sampling, testing, record keeping and incidentals necessary to complete the work.

HMA Pavement, Pavement Patching, Items SPV 460.1103 a-d

A.	Description.  The item of pavement patching is to be used for miscellaneous areas of wedging and patching around the County.  Materials covered under this provision shall conform to the State of Wisconsin, Department of Transportation's specifications for item 460.5224 - 4 LT 58-28 S.

B.	Basis of Payment.  HMA Pavement mixture of this type or types, accepted as stated above, shall be measured by the ton of mixed aggregate and asphaltic material laid and compacted in place and shall include all work necessary to provide quality management programs in accordance with QMP specifications listed in the bid documents.

C.	Method of Payment.  Payment will be made only for supplied material accompanied by a ticket containing the following information:

1.  Ticket number, date, and time

2.  Type of material

3.  Gross and net weights

A copy of the tickets will be given to the County inspector on the job site.

Partial payments will be made no sooner than monthly by the County as the work proceeds.  Final payment will be withheld until final acceptance is made by the County.

D.	Acceptance.  Final acceptance of all asphaltic mixes shall be based primarily on the overall quality of finished pavement, compacted densities, and the quality of workmanship.  Documentation of the contractor's quality management program are definite factors in determining final acceptance, however the County reserves the right to reject any pavement on the basis of an obvious inconsistency, poor appearance, or poor ride.

ASPHALTIC RUMBLE STRIPS, Item 465.0450

- Description.  This work shall consist of grinding rumble strips in the asphaltic pavement as hereinafter provided.

- Construction Methods.  The rumble strip area shall be constructed by grinding transverse "grooves" in the asphaltic pavement.  The "grooves" shall be 4-inches wide and 3/8-inch deep and be spaced one foot on center.  They will be cut transversely the same width as the lane along the centerline for 25 feet.  The grinding machine shall be a power operated, self-propelled machine having a cutting drum with a tooth pattern that will attain the desired pattern.  The grinding machine shall be equipped with a pressurized watering system for dust control and shall be of a type designed to perform this work.

Under this item, the County will supply the traffic control.  The contractor will notify the County 48 hours in advance of grinding in order for the County to provide traffic control.

- Method of Measurement.  Asphaltic Rumble Strips will be measured by each area.  An area will constitute a lane width, 25-feet long, with a completed grinding pattern as described above.

- Basis of Payment.  Rumble strips, measured as provided above, will be paid for at the contract unit price bid per each area for grinding, and shall be full compensation for grinding the existing pavement surface, preparation of the grinder, mobilization; and for furnishing all labor, tools, equipment and incidentals necessary to complete the work in accordance with this contract.

CONCRETE CURB AND GUTTER 24-Inch TYPE D SPECIAL, ITEM SPV.0090.01.

- Description  This special provision describes constructing concrete curb and gutter as shown in the plans in accordance to standard spec 601.

- (Vacant)

- (Vacant)

- Measurement  The department will measure Concrete Curb and Gutter 24-Inch Type D Special in accordance to standard spec 601.4.

- Payment  The department will pay for measured quantities at the contract unit price under the following bid item:

ITEM NUMBER	DESCRIPTION	UNIT

SPV.0090.01	Concrete Curb and Gutter 24-Inch Type D Special	LF

Payment is full compensation for furnishing all work, equipment, materials, labor, and incidentals required to complete the work as set for in the description.

CONCRETE DRIVEWAY 5-Inch, ITEM SPV.0095.01.

- Description  This special provision describes constructing concrete curb and gutter as shown in the plans in accordance to standard spec 416.

- (Vacant)

- (Vacant)

- Measurement  The department will measure Concrete Driveway 5-Inch Special in accordance to standard spec 416.4.

- Payment  The department will pay for measured quantities at the contract unit price under the following bid item:

ITEM NUMBER	DESCRIPTION	UNIT

SPV.0095.01	CONCRETE DRIVEWAY, 5-Inch	SY

Payment is full compensation for furnishing all work, equipment, materials, labor, and incidentals required to complete the work as set for in the description.

RAMPING MANHOLES CASTINGS, ITEM SPV.0100.01.

- Description  This special provision describes construction and removal of asphalt ramps around manhole castings.

- Materials  HMA used to ramp manholes shall conform to section 460 of the Standard Specifications

- Construction  Ramping SAS shall consist of cleaning the surface area around the casting, tacking the entire surface area to be wedged, placing hot mix asphalt mixture compacted to a depth within one-quarter (1/4) inch of the top of the adjusted casting and to a minimum radius width of one (1) foot for each one-half (1/2) inch of adjusted vertical height, and removal of ramping or as directed by the Engineer

- Measurement  Ramping manhole castings shall be measured as units of each.

- Payment  The unit price bid for ramping manhole castings shall include all costs for cleaning and tacking the surface to be wedged, supplying, placing, compacting hot mix asphalt mixture and removal as described above including finishing and protecting, and for all labor, tools, equipment and incidentals necessary to complete the work.

ITEM NUMBER	DESCRIPTION	UNIT

SPV.0100.01	RAMPING MANHOLE CASTINGS	EACH

Payment is full compensation for furnishing all work, equipment, materials, labor, and incidentals required to complete the work as set for in the description.

RAMPING SIDE ROADS, ITEM SPV.0105.01.

- Description  This special provision describes construction and removal of asphalt ramps at driveways and side roads.

- Materials  HMA used to ramp side roads shall conform to section 460 of the Standard Specifications.

- Construction  Ramping SAS shall consist of construction and removal of asphalt ramps along exposed but joints during paving of lower course.

- Measurement  Ramping driveways and side roads shall be measured per linear foot of ramp constructed along the side road butt joint.

- Payment  The unit price bid for ramping side roads shall include all costs for cleaning and tacking the surface to be wedged, supplying, placing, compacting hot mix asphalt mixture and removal as described above including finishing and protecting, and for all labor, tools, equipment and incidentals necessary to complete the work.

ITEM NUMBER	DESCRIPTION	UNIT

SPV.0100.01	RAMPING DRIVEWAYS & SIDE ROADS	LF

Payment is full compensation for furnishing all work, equipment, materials, labor, and incidentals required to complete the work as set for in the description.

MILLING, HOURLY, Item SPV.0180.2a, SPV0180.2b; 1-4’ Mill, 4+-12’ Mill respectively.

A.	Description.  This item is the same as Grinding, Item 204.0120, except as modified below.

B.	Traffic Control.  Under this item, the County will supply the traffic control.  The contractor will notify the County 48 hours in advance of grinding in order for the County to provide traffic control.

C.	Method of Measurement.  Grinding, Hourly, shall be measured in 1/2 hour increments of time spent on the job plus a fixed mobilization charge to the project site.  In the event of multiple projects there will be a fixed mobilization charge to the first project site, with an hourly charge starting when the mill unloads at the first project site and ending when the clean-up at the last project site is complete.

D.	Basis of Payment.  Grinding, Hourly will be paid for at the contract unit price bid for grinding, hourly and shall be full compensation for grinding the existing pavement surface, for wedging utility castings after grinding, for street cleaning, and for all equipment, tools, labor, and incidentals necessary to complete the work in accordance with this contract.

TRUCKING MILLED MATERIAL, HOURLY, Item SPV.0180.2c,

A.	Description.  This item is for trucking with quad-axel dump trucks and disposal of material produced by milling operations.

B.	Method of Measurement.  Trucking, Hourly, shall be measured in 1/2 hour increments of time spent on the job.  In the event of multiple projects time will start when the truck is loaded at the first project site and end when the truck leaves the last project site.

C.	Basis of Payment.  Trucking, Hourly, will be paid for at the contract unit price bid for trucking and shall be full compensation for the truck and operator and for all equipment, tools, labor, and incidentals necessary to complete the work in accordance with this contract.

MOBILIZATION, MILL, Item SPV.0180.3

- Description.  This section describes the work and operations necessary to move personnel, equipment, supplies and incidentals to the project site to accomplish grinding hourly operations.

- Method of Measurement.  Mobilization mill shall be measured as each individual unit acceptably completed.

- Basis of Payment.  Payment for mobilization mill is full compensation for supplying and providing all materials and services, and for performing all work necessary to complete this contract bid item.

Pulverized Pavement, Item SPV.0180.4

- Description.  This section describes full depth in-place milling/pulverizing of the existing asphaltic pavement along with a portion of the underlying base for the County to grade & shape.

- Construction.  Pulverize the full depth of the existing asphaltic pavement until 97 percent or more will pass the 2-inch (50 mm) sieve.  Also pulverize the existing base to the depth the plans show or as directed by the engineer.

- Measurement  Pulverize pavement will be measured by the square yard of asphalt pavement acceptably milled/pulverized, measured using the centerline length and the width from outside to outside of existing pavement.

- Basis of Payment.  The County will pay for the measured quantity at the contract unit price under the following item.  SPV.0180.4.  Payment is full compensation for pulverizing, mixing, and blending additional County-furnished base course and for furnishing all labor, equipment tools and incidentals necessary to complete the work as specified.  Cost for the addition of water shall be considered incidental to the item of pulverized pavement.

# SWEEPER RENTAL, SPV0180.5

GENERAL:  It is the intent of these specifications to describe the minimum requirements for the Rental of an Operated Sweeper Unit as follows:

- The unit must be an Elgin Crosswind J Recirculating Air Sweeper with 144 inch sweeping path or equal.

- The Sweeper must be operated by qualified personnel supplied by the contractor.

- Dane County will provide traffic control.

- Dane County will provide an area to dump the material.

- Dane County will provide water.

B.	Method of Measurement.  Sweeping, Hourly, shall be measured in 1/2 hour increments of time spent on the job.  The hourly charge starts when the sweeper is unloaded at the first project site and ending when the sweeper leaves the last project site.

C.	Basis of Payment.  Sweeping, Hourly, will be paid for at the contract unit price bid for sweeping and shall be full compensation for the sweeper and operator and for all equipment, tools, labor, and incidentals necessary to complete the work in accordance with this contract.

REMOVE AND REPLACE CONCRETE CURB & GUTTER – MACHINE PLACED ITEM SPV.0180.6; REMOVE AND REPLACE CONCRETE CURB & GUTTER – HAND PLACED ITEM SPV.0180.7

## Construction Methods.  The unit price bid for the various items listed in the proposal which involves removal and replacement of concrete curb and gutter shall include all costs for excavating curb and asphalt pavement, replacement of disturbed sub-base material with 3/4" crushed stone or crushed concrete, grade preparation, tree root removal, expansion joints and disposal.  If directed by the Engineer, "Type X" curb will be required at various locations at no additional cost.

The Contractor shall place all curb & gutter sections 100 feet and longer with the use of a slip form paver as directed by the Engineer except where obstructions prevent the uses of a machine.  Obstructions shall include but not be limited to:  inlets; sidewalk; castings and trees.

Removal of concrete curb and gutter shall include excavation of existing material including bituminous material, up to one (1) foot on each side of the curb and gutter, as the case may be.  All material shall be hauled from the site.  At no time shall any material be deposited on private property or terrace areas.

Existing concrete, bituminous mixes or other types of material used to shim raised curb & gutter shall be removed from adjacent curb & gutter stones prior to placing new curb & gutter.  All costs for said work to be included in the unit price bid for curb & gutter, as the case may be.

After the new curb and gutter has been constructed and the forms removed, the excavated areas adjacent to the curb and gutter shall be back filled immediately with the appropriate material; topsoil, crushed stone, concrete or bituminous mix.

All debris shall be removed from the excavated areas prior to placement of the topsoil.

The Contractor shall include all costs for transverse saw cuts at curb and gutter joints, where directed in the unit price for removal and replacement of concrete curb and gutter.

The Contractor shall construct the curb cuts using a "profile curb cut" with the curb head removed by using a machine type concrete saw specifically designed for this type of work.  The curb shall be cut off flush with the flow line through the ramp.  Profile curb cut shall be paid under BID ITEM 90006 – PROFILE CURB CUT.

The Contractor shall take precautions during construction operations not to disfigure, scar, or impair the health of any tree on public or private property.

The Contractor shall remove tree roots from existing live trees to an elevation of five inches (5") below the bottom of the concrete curb and gutter.  Cutting shall not be closer than two inches (2"), from the trunk of the tree.

Tree roots ends one-half inch (2") and up which are severed shall be cut with an axe, lopping shears or other means which will produce a clean cut on the same day of excavation.  The tree root ends shall be back filled with soil or other suitable means immediately following the cutting.

- Method of Measurement.  Concrete Curb and Gutter shall be measured by length in linear feet curb and gutter and shall exclude the distance through the inlets.

- Basis of Payment.  The contract unit price paid shall include fill, topsoil, seed and mulch.  Curb & Gutter placed with a slip form paver shall be paid under bid item SPV.0180.6 – Remove Existing Concrete Curb & Gutter and Construct Concrete Curb & Gutter – Machine Placed.  Curb & Gutter placed by hand shall be paid under bid item SPV.0180.7 – Remove Existing Concrete Curb & Gutter and Construct Concrete Curb & Gutter – Hand Placed.

REMOVE AND REPLACE CONCRETE SIDEWALK:  ITEM SPV.0180.10

## Construction Methods.  The unit price bid for the various items listed in the proposal which involves removal and replacement of concrete sidewalk and/or topsoil  shall include all costs for excavating, replacement of disturbed sub-base material with a granular or crushed stone base, grade preparation, tree root removal, expansion joints and disposal.

Removal of existing sidewalk shall include excavation of existing material to allow placement of forms.  All material shall be hauled from the site.  At no time shall any material be deposited on private property or terrace areas.

After the new sidewalk has been constructed and the forms removed, the excavated areas adjacent to the sidewalk shall be back filled immediately with the appropriate material; topsoil, crushed stone, concrete or bituminous mix.

All debris shall be removed from the excavated areas prior to placement of the topsoil.

The Contractor shall include all costs for transverse saw cuts at sidewalk joints, where directed in the unit price for removal and replacement of concrete sidewalk.

The Contractor shall construct the curb cuts using a "profile curb cut" with the curb head removed by using a machine type concrete saw specifically designed for this type of work.  The curb shall be cut off flush with the flow line through the ramp.  Profile curb cut shall be paid under BID ITEM 90006 – PROFILE CURB CUT.

The Contractor shall take precautions during construction operations not to disfigure, scar, or impair the health of any tree on public or private property.

The Contractor shall remove tree roots from existing live trees to an elevation of five inches (5") below the bottom of the concrete sidewalk.  Cutting shall not be closer than two inches (2"), from the trunk of the tree.

Tree roots ends one-half inch (2") and up which are severed shall be cut with an axe, lopping shears or other means which will produce a clean cut on the same day of excavation.  The tree root ends shall be back filled with soil or other suitable means immediately following the cutting.

- Method of Measurement.  Concrete sidewalk shall be measured by area (S.F.) of sidewalk removed, replaced and restored.

- Basis of Payment.  The contract unit price paid shall include fill, topsoil, seed and mulch.  Concrete sidewalk shall be paid under bid item SPV.0180.8 – Remove & Replace Concrete Sidewalk

Cold Mix Asphalt Pavement, Item SPV.0195.01.

- Description  This special provision describes the cold mix asphalt mixture design and constructing cold mix asphalt pavement.

- Materials

B1.	General  Furnish a homogeneous mixture that is in accordance to the pertinent requirements of section 460 of the standard specifications, except gradation which shall conform to the requirements listed below.

B.2	Aggregates  All aggregates to be used in the asphaltic mixtures shall be of virgin nature.  No recycled asphaltic aggregates will be accepted.  Ensure that the aggregate blend conforms to the gradation requirements in table B-1.  The values listed are design limits; production values may exceed those limits.

Table B-1 AGGREGATE GRADATION MASTER RANGE

| Sieve Size | Percent Passing |
| --- | --- |
| 1 in | 25 mm | 100 |
| ¾ in | 19 mm | 100 |
| ½ in | 12.5 mm | 90-100 |
| 3/8 in | 9.5 mm | 35-95 |
| No. 4 | 4.7 mm | 25-80 |
| No. 8 | 2.36 mm | 15-60 |
| No. 16 | 1.18 mm | 30-55 |
| No. 30 | 0.60 mm | 7-40 |
| No.50 | 0.30 mm | 5-25 |
| No. 100 | 0.15 mm |  |
| No. 200 | 0.075 mm | 3-8 |

B.3	Asphaltic Material  The asphaltic material shall be MC, SC, or Emulsified Asphalt conforming where applicable to section 455 of the standard specifications.  The liquid asphalt shall be mixed at a total rate of 5-7% by weight.  The exact rate shall be determined by the contractor to assure optimum performance.  The bitumen shall be mixed at the appropriate temperature for the particular grade.

B.4	Cold Mix Design  The contractor shall develop and submit an asphalt mix design as per the Asphalt Institute Manual MS-2 – Marshall Method.  Mix designs are to be submitted to the department a minimum of 2 weeks prior to paving for review.   The department will review mixture designs and report the results of that review to the contractor.

C.	Construction

C.1	Mixing Plant  The paving material shall be mixed in a plant equipped with weigh belt conveyer and automatic computer controlled proportioning of asphalt to aggregate.  The mixing chamber shall be a minimum of 85 inches long to insure complete and uniform mixing of the bitumen and aggregates.  The discharge temperature of the mix shall not exceed asphalt material manufacturer recommendations.  Cold mix must be produced and used in a continuous operation and may not be stockpiled to be used at a later date.

C.2	Preparation of Roadway  Prior to the application of the bituminous cold mix, the roadway is to be prepared conforming to section 211 of the standard specifications.  No tack coat shall be placed prior to placement of the asphalt mixture.

C.3	Asphaltic Mixture Paver  The paving material shall be laid with a self propelled paver conforming to section 450 of the standard specifications.

C.4	Compaction  The asphaltic mixture shall be compacted conforming to section 450.3.2.6.2.

D.	Measurement  The department will measure asphaltic mixtures by the ton of mixed aggregate and asphaltic material incorporated in the work unless the measurement subsection of a particular application specifies otherwise.  Provide the engineer with weigh tickets showing the net weight of each load of material delivered.  The department or department-authorized testing firms or agencies will test the contractor’s truck, storage silo, or plant scales.

- Payment  The department will pay for measured quantities at the contract unit price under the following bid item:

| ITEM NUMBER | DESCRIPTION | UNIT |
| --- | --- | --- |
| SPV.0195.01 | Cold Mix Asphalt Pavement | TON |

Payment is full compensation for providing cold mix asphalt mix designs; for preparing foundation; for furnishing, preparing, hauling, mixing, placing, and compacting mixture; and for all materials.

General Descriptions – Individual Projects

HMA Pavement for County and Municipal Projects

PRE-BID MEETING is scheduled on March 17, 2017 at 9:00 a.m. at 2302 Fish Hatchery Road, Madison, WI  53713.  Attendance by all bidders is optional, however bidders and subcontractors are strongly encouraged to attend.  There will be a brief presentation on the University Avenue “CTH MS” project to review staging plans and answer questions related to the project.

Questions related to other projects will be answered at the end of the University Avenue pre-bid meeting.  Any bidder questions after this date will need to be submitted in writing to the purchasing division.

CTH A (State Highway 92 to County Road PB) – Towns of Primrose & Montrose

Project No. 69198-1700

This project is broken into two sections.

- Section 1: STH 92 to Bridge east of Fritz Road – overlay and widen from 22 feet to 28 feet.

- Section 2: Bridge east of Fritz Road to CTH PB – Pulverize, Relay and pave 28 feet wide.

Prior to the contractors work Dane County will replace culverts, replace the bridge east of Fritz Road and bench and widen the existing gravel shoulders to accommodate the new 28 foot wide HMA surface.  Bridge replacement is anticipated to be completed in the fall of 2017.

Contractor work on Section 1 will include the following items:  Milling Butt Joints & HMA Pavement.  Milling Butt Joints includes the following locations.

- West End of the Project

- 2 @ Bridge near STH 92

- 2 Intersections

- 1 Driveway

Contractor work on Section 2 will include the following items:  Pulverized & Re-laid Pavement and HMA Pavement.  The existing pavement to be pulverized is 22 feet wide and the re-laid width will be 30 feet to accommodate the new 28 foot pavement.  The Pulverized & Re-laid bid item will be measured at 30 feet wide plus any additional area required at side roads and driveways and includes construction of overlap joint, butted joints (see detail drawing) to match existing pavement.  Tapered butt joints (see attached detail drawing) shall be a minimum of 50 feet long at each end of the project and as necessary to match side road paving.  Hauling of material to construct the butt joints will be incidental to the item of Pulverized and Re-laid Pavement.  Contractor is responsible for providing squared off butt joints which is incidental to construction.

Super-elevations in the pulverized area will be staked by Dane County.

Dane County will construct gravel shoulder after paving is completed.

The road will be open to traffic during construction.  The contractor is responsible for traffic control signing and flagging during their operations.  A minimum of two flaggers are required for all operations.  The contractors traffic control is incidental to construction.

Proposed Pavement Structure

| Pavement: | Scratch: 4 LT 58-28 S, Contractor may option 5 LT 58-28 S Lower: 4 LT 58-28 S Upper: 4 LT 58-28 S |
| --- | --- |
| Approx. Length | 92 to Fritz: 1.77 miles Fritz to PB: 2.77 miles |
| Width: | 92 to Fritz: 28 feet Fritz to PB: 28 feet |
| Depth: | 92 to Fritz: 1” Scratch 22’ wide plus 2 ¼” shoulder 6’ wide 1 ¾” Overlay 28’ wide Fritz to PB: 2” Lower, 2” Upper |

CTH CC (Ash Street to Railroad Overhead) Village of Oregon

Project No. 69073-1600

This project is a joint project between the Village of Oregon and Dane County to replace the existing water main, spot replacement of curb & gutter and reconstruct the pavement structure.

The Village of Oregon will let a separate contract to replace the water main and spot replace curb and gutter.  Dane County will excavate and prep the base at the completion of the water main project.

Contractor work on this project will include the following item:  HMA Pavement.  The HMA pavement will be constructed after Dane County completes roadway excavation and base prep.

CTH CC will be closed to thru traffic but open to local traffic during construction.  Dane County will be responsible for setting up the road closure and detour route.  The contractor is responsible for all other traffic control signing and flagging during their operations.  The contractors traffic control is incidental to construction.

Proposed Pavement Structure

| Pavement: | Lower 3 LT 58-28 S Upper 4 LT 58-28 S |
| --- | --- |
| Approx. Length: | 0.40 Miles |
| Width: | 30 feet |
| Depth: | Lower 3” Upper 2” |

CTH DM (Village of Dane North Limits to Morrisonville Road) – Towns Dane & Vienna

Project No. 69037-1700, CHIP FUNDED

This project is to construct a hot mix scratch overlay.  Dane County will replace culverts prior to the overlay and will construct gravel shoulders after contract work is complete.

Contractor work on this project will include the following items:  Removing Asphalt Surface Butt Joints & HMA Pavement.  Removing Asphalt Surface Butt Joints includes the following locations.

- East and West End of the Project

- 13 side roads

- 11 driveways

CTH DM will be open to traffic during construction.  The contractor is responsible for traffic control signing and flagging during their operations.  A minimum of two flaggers are required for all operations.  The contractors traffic control is incidental to construction.

Note:  Wisconsin DOT will be replacing the County Road DM bridge over the interstate in 2017.  During bridge construction County Road DM will be closed at the bridge but open to local traffic.  The WisDOT Construction date is not determined at this time.

Proposed Pavement Structure

| Pavement: | Scratch 4 LT 58-28 S, Contractor may option 5 LT 58-28 S Overlay 4 LT 58-28 S |
| --- | --- |
| Approx. Length: | 7.44 Miles |
| Width: | 22 feet |
| Depth: | 1” Scratch 1 3/4” Overlay |

CTH I (County Road V to County Road DM) Town of Vienna

Project No. 69173-1700

This project is to construct a hot mix scratch overlay.  Dane County will replace culverts prior to the overlay and will construct gravel shoulders after contract work is complete.

Contractor work on this project will include the following items:  Removing Asphalt Surface Butt Joints & HMA Pavement.  Removing Asphalt Surface Butt Joints includes the following locations.

- North and South End of the project

- North and South End of the I39 bridge reconstruction project

- 3 side roads

- 4 driveways

CTH I will be open to traffic during construction.  The contractor is responsible for traffic control signing and flagging during their operations.  A minimum of two flaggers are required for all operations.  The contractors traffic control is incidental to construction.

Note:  County Road I will be the detour route for the County Road DM Project during WisDOT reconstruction of the DM Bridge over the Interstate.

Proposed Pavement Structure

| Pavement: | Scratch 4 LT 58-28 S, Contractor may option 5 LT 58-28 S Overlay 4 LT 58-28 S |
| --- | --- |
| Approx. Length: | 1.31 Miles |
| Width: | 28 feet |
| Depth: | 1” Scratch 2” Overlay |

University Ave “CTH MS” (Allen Blvd to Park Street) City of Middleton, Project No. 69039-1700

This project is to remove the existing concrete pavement, asphalt pavement, concrete curb & gutter, base and subgrade and construct a new base, concrete curb and gutter and HMA pavement.  Excavation work on this project is anticipated to begin in Mid to late April.

Dane County will excavate the existing base and subgrade, reconstruct storm sewer as necessary, construct new base course and landscape/finish the project.

The Contractor work on this project will include the following items:  Removing Pavement, Removing Asphaltic Surface, Removing Curb and Gutter; and to construct new Concrete Curb & Gutter, Concrete Median Sloped Nose, Concrete Driveway, Concrete Sidewalk and 6” HMA Pavement.  The roadway will be constructed in 4 main phases as shown on the plans and will include 4 interim phases for the construction of the Branch Street and Park Street intersections.  Contractor mobilization for each phase is incidental to construction.

Phase 1:  550 feet east of Allen Blvd. to Branch Street “North ½ of Road”:  Dane County will install traffic control to shift thru traffic to the existing eastbound lanes.  West of Branch Street traffic will continue to use the existing lane configuration.

The contractor will remove concrete pavement, concrete drive aprons and curb and gutter along the north ½ of the street.  Concrete removals will end just east of the Branch Street intersection.  Dane County will work behind the contractor excavating subgrade and constructing new base coarse up to Branch Street.  At completion of base work by Dane County the contractor will construct the concrete curb and gutter, concrete sidewalk and driveway aprons (see notes specific to access points below).  Dane County will finish the base and construct phase 1a as soon as curb work is complete in preparation for the contractor to construct the HMA pavement lower course.  Dane County will notify the contractor 3 days before paving is anticipated to begin and the contractor must begin paving within one day of the County finishing grade work.  Paving is to include temporary ramps at side roads and around manholes during binder operations.

Phase 1a:  After concrete curb and driveway work is complete, Dane County will remove the concrete pavement in the east ½ of the Branch Street intersection, excavate the subgrade and construct the new base.  This will be done as blitz construction and the contractor shall begin paving operations to construct binder in the intersection within 24 hours of the County finishing their operations.  Any remaining binder paving from phase 1 is to be completed in conjunction with this work.

Phase 2:  550 feet east of Allen Blvd to Branch Street “South ½ of Road”.  Dane County will shift both lanes of traffic onto the new lower pavement course constructed in Stage 1.  West of Branch Street traffic will continue to use the existing pavement configuration.

County and Contractor operations will mirror the description from Phase 1.  At the completion of lower course paving the upper course will be paved from Allen Blvd. to just east of Mendota Avenue.  Phase 2 upper course pavement will be constructed on the closed section from phase 2.  After this is completed Dane County will install permanent pavement marking and switch eastbound traffic onto the new pavement.  Once the traffic is switched the County will remove traffic delineators from phase 1 and the contractor is to pave the upper course under traffic.

No upper course pavement will be placed in the Mendota Avenue and Branch street intersections.  This will allow for installation of temporary traffic control for the crossovers used in Phases 3 & 4.

Phase 3:  Branch Street to 450 feet west of Park Street “North ½ of Road”.  Dane County will install traffic control to shift thru traffic to the existing eastbound lanes.

The contractor will remove concrete pavement, concrete drive aprons and curb and gutter along the north ½ of the street.  Concrete removals will gap the Park Street intersection which will be constructed in separate phases.  West of the median past park street Dane County will saw cut the existing pavement 3’ north of the road centerline.  This will allow a 3’ buffer zone to be left in place during the concrete removal.  Dane County will work behind the contractor excavating subgrade and constructing new base coarse behind contractor removal operations.  At completion of base work by Dane County the contractor will construct the concrete curb and gutter, concrete sidewalk and driveway aprons (see notes specific to access points below).  Dane County will finish the base and construct phase 3a as soon as curb work is complete in preparation for the contractor to construct the HMA pavement lower course.  Dane County will notify the contractor 3 days before paving is anticipated to begin and the contractor must begin paving within one day of the County finishing grade work.  Paving is to include temporary ramps at side roads and around manholes during binder operations.

Phase 3a:  After concrete curb and driveway work is complete, Dane County will close the north ½ of the Park Street intersection, remove the concrete pavement, excavate the subgrade and construct the new base.  This will be done as blitz construction and the contractor shall begin paving operations to construct binder in the intersection within 24 hours of the County finishing their operations.  Any remaining binder paving from phase 3 is to be completed in conjunction with this work.

Phase 4:  Branch Street to 450 feet west of Park Street “South ½ of Road”.  Dane County will install traffic control to shift thru traffic to the new lower pavement course.

Contractor and County operations will mirror the description from Phase 3.

Phase 4a:  This work will mirror the description in section 3a.  Upper course paving can be completed on the closed section of phase 4 and under traffic on the remainder of the project.

Business Access must be maintained at all times during removals and construction of concrete curbs and driveway aprons.  Short term closures during HMA paving operations will be allowed.  Businesses with a single access point must be constructed ½ at a time.  Businesses with two (2) access points must have at least one access left open at all times.  The contractor will need to coordinate with Dane County construction crews to have crushed aggregate stockpiled on the job site for the contractor to ramp access points during removal operations.  Ramping of drives during removal will be considered incidental to the removal item.  Dane County will be responsible for future maintenance of access points.  See Attached City of Middleton Standard Detail Drawing 600-4 for commercial driveway apron construction details.

Residential Access may be temporarily closed during construction operations by notification to the property owner.  During excavation these closures will be limited to the time the construction is occurring immediately in front of the property.  The contractor will need to coordinate with Dane County construction crews to have crushed aggregate stockpiled on the job site for the contractor to ramp access points during removal operations.  Ramping of drives during removal will be considered incidental to the removal item.  During concrete curb and concrete driveway operations the contractor may close these driveways for up to 7 days total to include both the curb and driveway apron. See Attached City of Middleton Standard Detail Drawing 600-3 for residential driveway apron construction details.

Concrete Safety Island is to be constructed as shown in the proposed typical section with 10’ turn lane.

Traffic Control:  Dane County will be responsible for installation and maintenance of permanent traffic control.  The contractor will be responsible to replace permanent traffic control drums and barricades moved during their operations. In addition, the contractor will also be responsible for temporary signing required for their operation and flaggers to direct traffic around their operation during construction.  Contractor traffic control is incidental to construction.

Proposed Pavement Structure

| Pavement: | Lower: 3 MT 58-28 S Upper: 4 MT 58-28 S |
| --- | --- |
| Approx. Length: | 0.96 Miles |
| Width: | See typical sections plan sheets |
| Depth: | 4” Lower 2” Upper |

Attached Drawings:

- Plan Sheets

- Traffic Staging Sheets

- Curb ramp Types 1 & 2 detail drawing

- Residential Driveway Apron Detail

- Commercial Driveway Apron Detail

- Concrete Curb & Gutter, 24-Inch Type D, Special Detail

CTH N (County Road B “east” to approx. 1,000 feet north of Koshkonong Road)

Town of Pleasant Springs

CTH N (Approximately 1000 feet north of Rinden Road to US Highway 12/18)

Towns of Pleasant Springs & Cottage Grove

Project Nos. 69040-1700 & 69199-1700 Respectively

This project is to mill the existing pavement and construct a new 5” HMA pavement.  The work will be let as individual projects but both projects will be awarded to the low bidder of the combined projects.

Contractor work on this project will include the following items:  Removing Asphaltic Surface and HMA pavement.  Mill 3 ½” at the centerline at a 2 ½% cross slope.  The new pavement will be constructed at 2 ½% cross slope to match the milled slope.  Lower course pavement must be placed on the same day as milling and may progress in one lane for an entire day.  The contractor must backup to mill & pave the adjacent lane the next day.

Removing Asphalt Surface will include the widened pavement areas at US 12 and will be measured and paid at the width required to remove the existing asphalt pavement only.  Additional milling wider than the pavement to accommodate paving operations will be incidental to the item removing asphalt surface milling.

Dane County will construct gravel shoulders after contract work is complete.

CTH N will be open to traffic during construction.  The contractor is responsible for traffic control signing (including uneven pavement signs as necessary) and flagging during their operations.  A minimum of two flaggers are required for all operations.  The contractors traffic control is incidental to construction.

Note:  CTH N between the two project areas listed above will be under construction as part of the WisDOT I39 interchange project starting in May of 2017 and extending through the summer.  The contractor will be responsible for determining access to each project location, coordinating work with the WisDOT construction and proper signing to avoid conflicts with WisDOT construction.

Proposed Pavement Structure

| Pavement: | Lower: 3 MT 58-28 S Upper: 4 MT 58-28 S |
| --- | --- |
| Approx. Length: | B “east” to 1,000’ N. of Koshkonong - 2.25 miles 1,000’ N of Rinden to US 12/18 - 1.64 miles |
| Width: | 30 feet |
| Depth: | 3” Lower 2” Upper |

CTH O (CTH BB to North 3,250 feet to the East County Line) – Town of Deerfield

Project No. 69041-1700

This project is to construct a hot mix scratch overlay.  Dane County will replace culverts prior to the overlay and will construct gravel shoulders after contract work is complete.

Contractor work on this project will include the following items:  Removing Asphalt Surface Butt Joints & HMA Pavement.  Removing Asphalt Surface Butt Joints includes the following locations.

- North and South End of the Project

- 3 driveways

The road will be open to traffic during construction.  The contractor is responsible for traffic control signing and flagging during their operations.  A minimum of two flaggers are required for all operations.  The contractors traffic control is incidental to construction.

Proposed Pavement Structure

| Pavement: | Scratch: 4 LT 58-28 S, Contractor may option 5 LT 58-28 S Overlay: 4 LT 58-28 S |
| --- | --- |
| Approx. Length: | 0.62 Miles |
| Width: | 22 feet |
| Depth: | 1” Scratch 1 3/4” Overlay |

CTH Y (0.37 Miles north of Amenda Road to STH 78) – Town Mazomanie

Project No. 69042-1700, CHIP Funded

This project is to construct a cold mix overlay.  Prior to the contractors work the County will replace culverts and bench and widen the existing gravel shoulders to accommodate the new 28 foot wide pavement.

Contractor work on this project will include the following items:  Removing Asphalt Surface Butt Joints & Asphaltic Cold Mix Pavement.  Removing Asphalt Surface Butt Joints includes the following locations.

- North and South End of the Project

- Bridge approaches

- 12 side roads

- 6 driveways

CTH Y will be open to traffic during construction.  The contractor is responsible for traffic control signing and flagging during their operations.  A minimum of two flaggers are required for all operations.  The contractors traffic control is incidental to construction.

Proposed Pavement Structure

| Pavement: | Overlay: Cold Mix Pavement |
| --- | --- |
| Approx. Length: | 5.86 Miles |
| Width: | 30 feet |
| Depth: | 3” x 22’ Overlay 5” x 8’ Widening (4 feet each side) |

Specification Deviations

Check One:

(  Deviations – No deviations from specs

(  Deviations – See list below

Item #		Deviation Explanation

________ _______________________________________________________________ ________ _______________________________________________________________ ________ _______________________________________________________________ ________ _______________________________________________________________ ________ _______________________________________________________________ ________ _______________________________________________________________ ________ _______________________________________________________________ ________ _______________________________________________________________ ________ _______________________________________________________________ ________ _______________________________________________________________ ________ _______________________________________________________________ ________ _______________________________________________________________ ________ _______________________________________________________________ ________ _______________________________________________________________ ________ _______________________________________________________________ ________ _______________________________________________________________

###### Part 3 – Detailed Specifications

###### Submit with Bid

ATTACHMENTS

# There are three (3) attachments associated with this bid document. The attachments can be found and downloaded from the Dane County Purchasing Website, www.danepurchasing.com

# .

# Attachment 1 – Overlap Joint, Butted Detail – CTH A

# Attachment 2 – University Ave – Traffic Staging

# Attachment 3 – University Ave – Plan View and Detail Sheets

# Part 4 – Price Proposal

Submit With Bid

| PRICE PROPOSAL |
| --- |
| NAME OF COMPANY: |  |

For the price(s) listed below, our company hereby offers to provide the following item(s) in accordance with the specifications of this bid. Pricing must include delivery.

CTH A (State Highway 92 to County Road PB) – Towns of Primrose & Montrose

Project No. 69198-1700

| Item No. | Approx. Quantity | Item |  | Unit Bid |  | Net Bid |
| --- | --- | --- | --- | --- | --- | --- |
| 204.0120 | 355 | REMOVING ASPHALT |  |  |  |  |
|  | SY | SURFACE MILLING | $ |  | $ |  |
| 325.0100 | 48,833 | PULVERIZED & RE-LAID |  |  |  |  |
|  | SY | PAVEMENT | $ |  | $ |  |
| 455.0605 | 4,900 | ASPHALTIC MATERIAL |  |  |  |  |
|  | GAL | FOR TACK COAT | $ |  | $ |  |
| 460.5224 | 5,350 | HMA PAVEMENT |  |  |  |  |
|  | TON | 4 LT 58-28 S, LOWER CRSE. | $ |  | $ |  |
| 460.5224 | 10,250 | HMA PAVEMENT |  |  |  |  |
|  | TON | 4 LT 58-28 S, UPPER COURSE | $ |  | $ |  |
| 649.0300 | 1,000 | TEMP PAVEMENT MARKING |  |  |  |  |
|  | LF | 4-INCH, REFLECTIVE TAPE | $ |  | $ |  |
|  |  | TOTAL BID |  |  | $ |  |

Part 4 – Price Proposal

Submit With Bid

| PRICE PROPOSAL |
| --- |
| NAME OF COMPANY: |  |

For the price(s) listed below, our company hereby offers to provide the following item(s) in accordance with the specifications of this bid. Pricing must include delivery.

CTH CC (Ash Street to Railroad Overhead) Village of Oregon

Project No. 69073-1600

| Item No. | Approx. Quantity | Item |  | Unit Bid |  | Net Bid |
| --- | --- | --- | --- | --- | --- | --- |
| 455.0605 | 350 | ASPHALTIC MATERIAL |  |  |  |  |
|  | GAL | FOR TACK COAT | $ |  | $ |  |
| 460.5223 | 1,320 | HMA PAVEMENT |  |  |  |  |
|  | TON | 3 LT 58-28 S, LOWER CRSE. | $ |  | $ |  |
| 460.5224 | 880 | HMA PAVEMENT |  |  |  |  |
|  | TON | 4 LT 58-28 S, UPPER COURSE | $ |  | $ |  |
|  |  | TOTAL BID |  |  | $ |  |

Part 4 – Price Proposal

Submit With Bid

| PRICE PROPOSAL |
| --- |
| NAME OF COMPANY: |  |

For the price(s) listed below, our company hereby offers to provide the following item(s) in accordance with the specifications of this bid. Pricing must include delivery.

CTH DM (Village of Dane North Limits to Morrisonville Road) – Towns Dane & Vienna

Project No. 69037-1700

| Item No. | Approx. Quantity | Item |  | Unit Bid |  | Net Bid |
| --- | --- | --- | --- | --- | --- | --- |
| 204.0120 | 925 | REMOVING ASPHALT |  |  |  |  |
|  | SY | SURFACE BUTT JOINT | $ |  | $ |  |
| 455.0605 | 9,600 | ASPHALTIC MATERIAL |  |  |  |  |
|  | GAL | FOR TACK COAT | $ |  | $ |  |
| 460.5224 | 15,500 | HMA PAVEMENT |  |  |  |  |
|  | TON | 4 LT 58-28 S, UPPER COURSE | $ |  | $ |  |
| 649.0300 | 1,575 | TEMP PAVEMENT MARKING |  |  |  |  |
|  | LF | 4-INCH, REFLECTIVE TAPE | $ |  | $ |  |
|  |  | TOTAL BID |  |  | $ |  |

Part 4 – Price Proposal

Submit With Bid

| PRICE PROPOSAL |
| --- |
| NAME OF COMPANY: |  |

For the price(s) listed below, our company hereby offers to provide the following item(s) in accordance with the specifications of this bid. Pricing must include delivery.

CTH I (County Road V to County Road DM) Town of Vienna

Project No. 69173-1700

| Item No. | Approx. Quantity | Item |  | Unit Bid |  | Net Bid |
| --- | --- | --- | --- | --- | --- | --- |
| 204.0120 | 500 | REMOVING ASPHALT |  |  |  |  |
|  | SY | SURFACE BUTT JOINT | $ |  | $ |  |
| 455.0605 | 2,200 | ASPHALTIC MATERIAL |  |  |  |  |
|  | GAL | FOR TACK COAT | $ |  | $ |  |
| 460.5224 | 4,000 | HMA PAVEMENT |  |  |  |  |
|  | TON | 4 LT 58-28 S, UPPER COURSE | $ |  | $ |  |
| 649.0300 | 380 | TEMP PAVEMENT MARKING |  |  |  |  |
|  | LF | 4-INCH, REFLECTIVE TAPE | $ |  | $ |  |
|  |  | TOTAL BID |  |  | $ |  |

Part 4 – Price Proposal

Submit With Bid

| PRICE PROPOSAL |
| --- |
| NAME OF COMPANY: |  |

For the price(s) listed below, our company hereby offers to provide the following item(s) in accordance with the specifications of this bid. Pricing must include delivery.

University Ave “CTH MS” (Allen Blvd to Park Street) City of Middleton, Project No. 69039-1700

| Item No. | Approx. Quantity | Item |  | Unit Bid |  | Net Bid |
| --- | --- | --- | --- | --- | --- | --- |
| 204.0100 | 31,700 | REMOVING PAVEMENT |  |  |  |  |
|  | SY |  | $ |  | $ |  |
| 204.0110 | 4,000 | REMOVING ASPHALTIC |  |  |  |  |
|  | SY | SURFACE | $ |  | $ |  |
| 204.0150 | 13,500 | REMOVING CURB & GUTTER |  |  |  |  |
|  | LF |  | $ |  | $ |  |
| 204.0155 | 700 | REMOVING CONCRETE |  |  |  |  |
|  | SY | SIDEWALK | $ |  | $ |  |
| 416.0170 | 1,200 | CONCRETE DRIVEWAY |  |  |  |  |
|  | SY | 7-INCH | $ |  | $ |  |
| 455.0605 | 1,600 | ASPHALTIC MATERIAL |  |  |  |  |
|  | GAL | FOR TACK COAT | $ |  | $ |  |
| 460.6223 | 8,000 | HMA PAVEMENT |  |  |  |  |
|  | TON | 3 MT 58-28 S, LOWER CRSE. | $ |  | $ |  |
| 460.6224 | 4,000 | HMA PAVEMENT |  |  |  |  |
|  | TON | 4 MT 58-28 S, UPPER CRSE. | $ |  | $ |  |
| 601.0407 | 2,900 | CONCRETE CURB & GUTTER |  |  |  |  |
|  | LF | 18-INCH, TYPE D | $ |  | $ |  |
| 601.0411 | 7,100 | CONCRETE CURB & GUTTER |  |  |  |  |
|  | LF | 30-INCH, TYPE D | $ |  | $ |  |
| 602.0410 | 6,500 | CONCRETE SIDEWALK, |  |  |  |  |
|  | SF | 5-INCH | $ |  | $ |  |
| 602.0420 | 150 | CONCRETE SIDEWALK, |  |  |  |  |
|  | SF | 7-INCH | $ |  | $ |  |
|  |  | Continued on next page |  |  |  |  |
| University Ave “CTH MS” (Allen Blvd to Park Street) City of Middleton |
| Item No. | Approx. Quantity | Item |  | Unit Bid |  | Net Bid |
| 602.0505 | 310 | CURB RAMP DETECTABLE |  |  |  |  |
|  | SF | WARNING FIELD, YELLOW | $ |  | $ |  |
| 602.2400 | 1,580 | CONCRETE SAFETY |  |  |  |  |
|  | SF | ISLAND | $ |  | $ |  |
| 620.0300 | 700 | CONCRETE MEDIAN |  |  |  |  |
|  | SF | SLOPED NOSE | $ |  | $ |  |
| 649.0300 | 380 | TEMP PAVEMENT MARKING |  |  |  |  |
|  | LF | 4-INCH, REFLECTIVE TAPE | $ |  | $ |  |
| SPV.0090.01 | 2,440 | CONCRETE CURB & GUTTER |  |  |  |  |
|  | LF | 24-INCH, TYPE D, SPECIAL | $ |  | $ |  |
| SPV.0095.01 | 80 | CONCRETE DRIVEWAY |  |  |  |  |
|  | SY | 5-INCH | $ |  | $ |  |
| SPV.0100.01 | 16 | RAMPING MANHOLE |  |  |  |  |
|  | EACH | CASTINGS | $ |  | $ |  |
| SPV.0105.01 | 250 | RAMPING SIDE ROADS |  |  |  |  |
|  | LF |  | $ |  | $ |  |
|  |  | TOTAL BID |  |  | $ |  |

Part 4 – Price Proposal

Submit With Bid

Part 4 – Price Proposal

Submit With Bid

| PRICE PROPOSAL |
| --- |
| NAME OF COMPANY: |  |

For the price(s) listed below, our company hereby offers to provide the following item(s) in accordance with the specifications of this bid. Pricing must include delivery.

CTH N (County Road B “east” to approx. 1,000 feet north of Koshkonong Road)

Town of Pleasant Springs

Project No. 69040-1700

| Item No. | Approx. Quantity | Item |  | Unit Bid |  | Net Bid |
| --- | --- | --- | --- | --- | --- | --- |
| 204.0120 | 40,000 | REMOVING ASPHALT |  |  |  |  |
|  | SY | SURFACE MILLING | $ |  | $ |  |
| 455.0605 | 2,000 | ASPHALTIC MATERIAL |  |  |  |  |
|  | GAL | FOR TACK COAT | $ |  | $ |  |
| 460.6223 | 6,800 | HMA PAVEMENT |  |  |  |  |
|  | TON | 3 MT 58-28 S, LOWER CRSE. | $ |  | $ |  |
| 460.6224 | 4,500 | HMA PAVEMENT |  |  |  |  |
|  | TON | 4 MT 58-28 S, UPPER CRSE. | $ |  | $ |  |
| 649.0300 | 500 | TEMP. PAVMENT MARKING, |  |  |  |  |
|  | LF | 4-INCH, REFLECTIVE TAPE | $ |  | $ |  |
|  |  | TOTAL BID |  |  | $ |  |

Part 4 – Price Proposal

Submit With Bid

| PRICE PROPOSAL |
| --- |
| NAME OF COMPANY: |  |

For the price(s) listed below, our company hereby offers to provide the following item(s) in accordance with the specifications of this bid. Pricing must include delivery.

CTH N (Approximately 1000 feet north of Rinden Road to US Highway 12/18)

Towns of Pleasant Springs & Cottage Grove

Project No. 69199-1700

| Item No. | Approx. Quantity | Item |  | Unit Bid |  | Net Bid |
| --- | --- | --- | --- | --- | --- | --- |
| 204.0120 | 30,500 | REMOVING ASPHALT |  |  |  |  |
|  | SY | SURFACE MILLING | $ |  | $ |  |
| 455.0605 | 1,500 | ASPHALTIC MATERIAL |  |  |  |  |
|  | GAL | FOR TACK COAT | $ |  | $ |  |
| 460.6223 | 5,200 | HMA PAVEMENT |  |  |  |  |
|  | TON | 3 MT 58-28 S, LOWER CRSE. | $ |  | $ |  |
| 460.6224 | 3,400 | HMA PAVEMENT |  |  |  |  |
|  | TON | 4 MT 58-28 S, UPPER CRSE. | $ |  | $ |  |
| 649.0300 | 350 | TEMP. PAVMENT MARKING, |  |  |  |  |
|  | LF | 4-INCH, REFLECTIVE TAPE | $ |  | $ |  |
|  |  | TOTAL BID |  |  | $ |  |

Part 4 – Price Proposal

Submit With Bid

| PRICE PROPOSAL |
| --- |
| NAME OF COMPANY: |  |

For the price(s) listed below, our company hereby offers to provide the following item(s) in accordance with the specifications of this bid. Pricing must include delivery.

CTH O (CTH BB to North 3,250 feet to the East County Line) – Town of Deerfield

Project No. 69041-1700

| Item No. | Approx. Quantity | Item |  | Unit Bid |  | Net Bid |
| --- | --- | --- | --- | --- | --- | --- |
| 204.0120 | 150 | REMOVING ASPHALT |  |  |  |  |
|  | SY | SURFACE MILLING | $ |  | $ |  |
| 455.0605 | 650 | ASPHALTIC MATERIAL |  |  |  |  |
|  | GAL | FOR TACK COAT | $ |  | $ |  |
| 460.5224 | 1,265 | HMA PAVEMENT |  |  |  |  |
|  | TON | 4 LT 58-28 S, UPPER COURSE | $ |  | $ |  |
| 649.0300 | 70 | TEMP. PAVMENT MARKING, |  |  |  |  |
|  | LF | 4-INCH, REFLECTIVE TAPE | $ |  | $ |  |
|  |  | TOTAL BID |  |  | $ |  |

Part 4 – Price Proposal

Submit With Bid

| PRICE PROPOSAL |
| --- |
| NAME OF COMPANY: |  |

For the price(s) listed below, our company hereby offers to provide the following item(s) in accordance with the specifications of this bid. Pricing must include delivery.

CTH Y (0.37 Miles north of Amenda Road to STH 78) – Town Mazomanie

Project No. 69042-1700

| Item No. | Approx. Quantity | Item |  | Unit Bid |  | Net Bid |
| --- | --- | --- | --- | --- | --- | --- |
| 204.0120 | 870 | REMOVING ASPHALT |  |  |  |  |
|  | SY | SURFACE MILLING | $ |  | $ |  |
| 455.0605 | 3,700 | ASPHALTIC MATERIAL |  |  |  |  |
|  | GAL | FOR TACK COAT | $ |  | $ |  |
| SPV.0195.01 | 20,550 | ASPHALTIC COLD MIX |  |  |  |  |
|  | TON | SURFACING | $ |  | $ |  |
| 649.0300 | 620 | TEMP. PAVMENT MARKING, |  |  |  |  |
|  | LF | 4-INCH, REFLECTIVE TAPE | $ |  | $ |  |
|  |  | TOTAL BID |  |  | $ |  |

Part 4 – Price Proposal

Submit With Bid

| PRICE PROPOSAL |
| --- |
| NAME OF COMPANY: |  |

For the price(s) listed below, our company hereby offers to provide the following item(s) in accordance with the specifications of this bid. Pricing must include delivery.

Milling and Pavement Patching

###### Various Locations, Dane County

| Item No. | Approximate Quantity | Item |  | Unit Bid |
| --- | --- | --- | --- | --- |
| 455.0605 |  | ASPHALTIC MATERIAL |  |  |
|  |  | FOR TACK COAT (PER GAL.) | $ |  |
| SPV | 0-50 | PAVEMENT PATCHING |  |  |
| 460.1103a | Tons | ASPHALTIC CONC. PAVEMENT |  |  |
|  |  | 4 LT 58-28 S, UPPER COURSE | $ |  |
| SPV | 50-100 | PAVEMENT PATCHING |  |  |
| 460.1103b | Tons | ASPHALTIC CONC. PAVEMENT |  |  |
|  |  | 4 LT 58-28 S, UPPER COURSE | $ |  |
| SPV | 100-400 | PAVEMENT PATCHING |  |  |
| 460.1103c | Tons | ASPHALTIC CONC. PAVEMENT |  |  |
|  |  | 4 LT 58-28 S, UPPER COURSE | $ |  |
| SPV | 400+ | PAVEMENT PATCHING |  |  |
| 460.1103d | Tons | ASPHALTIC CONC. PAVEMENT |  |  |
|  |  | 4 LT 58-28 S, UPPER COURSE | $ |  |
| SPV.0180.2a |  | MILLING, 1-4’ WIDTH |  |  |
|  |  | (PER HOUR) | $ |  |
| SPV.0180.2b |  | MILLING, 4+-12’ WIDTH |  |  |
|  |  | (PER HOUR) | $ |  |
| SPV.0180.2c |  | TRUCKING |  |  |
|  |  | (PER HOUR) | $ |  |
| SPV.0180.3 | 1 | MOBILIZATION, MILL |  |  |
|  | LS | (PER EACH) | $ |  |

Part 4 – Price Proposal

Submit With Bid

| PRICE PROPOSAL |
| --- |
| NAME OF COMPANY: |  |

For the price(s) listed below, our company hereby offers to provide the following item(s) in accordance with the specifications of this bid. Pricing must include delivery.

Sweeping Various Locations

State, County and Local Roads

| Item No. | Approximate Quantity | Item |  | Unit Bid |  |
| --- | --- | --- | --- | --- | --- |
| SPV 180.5 |  | Sweeper Rental (see specs) |  |  |  |
|  |  | (per Hr) | $ |  |  |

The following questionnaire must be filled in completely.

1.  Make:            ____________________________________________

Model:           ____________________________________________

2. Rated capacity:  ______________________ cubic yards